No. 2629-OT Broadway Litter Container with Open TopPRIVATE 

Litter Container shall be TimberForm® Broadway( series model No. 2629-OT 2'-2" diameter, in the color finish and mounting style selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings. Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue Suite 310, Portland, OR 97201-3464 U.S.A.

1.  Materials

Top and bottom ring shall be fabricated from 1-1/4 inch i.d. schedule 40 mild steel pipe. Thin wall tubing shall not be permitted. Bottom plate shall be 1/4 inch steel plate, and upper support frame shall be 1/4 inch curved steel bar. Sides shall be laser cut from smooth 3/16 inch thick curved steel sheet. Litter container shall include a 32-gallon plastic liner.  Separate mounting hardware shall be -L leveling (moveable), -P pedestal (fixed leveling) or -E embedded (permanent) as selected by the owner's representative.  Leveling (-L) hardware shall be fitted with non-marring UHMW pads.

2.  Construction

Entire litter container unit, except for separate liner and mounting hardware, shall be assembled and welded into a single unit.  Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3.  Finish

Steel parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.   

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.  

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.

© 2004 Columbia Cascade Company.  No portion of this publication may be reproduced without prior authorization.  Authorization is hereby granted for photocopies to

                    be made and distributed to those involved in the specification of TimberForm products.


