No. 2942 Profile Square Table with Center Support

Square Table with Center Support shall be TimberForm® Profile( series model No. 2942 in the size, color finish and mounting style selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings. Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue Suite 310, Portland, OR 97201-3464 U.S.A.

1.  Materials

Post and support beam shall be fabricated from 4 inch i.d. schedule 40 mild steel seamless pipe.  Top frame shall be fabricated from 3/4 inch i.d. schedule 40 mild steel seamless pipe.  Table surface shall be fabricated from 1 inch x 1 inch x 1/8 inch welded wire grid.  Square table top shall be 30 inch, 36 inch or 42 inch square.  No. 2095 GameBoard (2943) and umbrella hole (2944) optional. Mounting shall be -P (pedestal) or -E embedment (permanent).

2.  Construction

Top frame, wire grid, post, and beam shall be permanently welded into a single unit. Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.

3.  Finish

Steel parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.   

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.  

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.
© 2010 Columbia Cascade Company.  No portion of this publication may be reproduced without prior authorization.  Authorization is hereby granted for photocopies to be made and distributed to those involved in the specification of TimberForm products.

